SOLUTIONS PLUS CHEMICAL DATA

ALUMA WASH RR

POWDERED MULTI-METAL CLEANER

BENEFITS

1. Effective at very low and at high concentrations.

2. Stable in all water conditions.

3. Economical to use.

4. Versatility - multi metal applications.

GENERAL DESCRIPTION

ALUMA WASH RR is a specially formulated powdered mixture designed for use in spray washers where a variety of metals are being processed.  It is free rinsing and readily emulsifies a variety of process oils and grease occurring on metal being processed - engine parts, baking pans, etc.

PROPERTIES

Appearance:						White to cream powder

Odor:							Characteristic

Wetting:						Excellent

Phosphates:						Present

Biodegradable:					Yes - all surfactants

MATERIAL SAFETY

ALUMA WASH RR is safe on most soft metals.  At normal use dilutions, it is safe on aluminum, nickel, cast iron, steel, galvanize stainless steel.

USE DIRECTIONS

Use ALUMA WASH RR at concentrations ranging from 1/2 once to

16 onces/gallon.  Soil type and degree of soiling usually determine product concentration.  The temperature range for most jobs should be 110 F and 170F.  Jobs may be sprayed or dipped.  Exposure to products is normally followed by a warm to hot water rinse and other processes (rust inhibition, etc.).