Registered ISO 9001:2008 Manufacturer

INDUSTRIAL CHEMICAL PRODUCTS

Quality-Cost Savings-Service

CLG-1

CLG-1 Grease is a premium, heavy duty, multi-purpose lithium complex grease specially designed for both low and high temperature performance.  This high melting point grease is enhanced with special additives to give it very high film strength, anti-wear and EP performance.  It incorporates premium quality high flash point oils and combines them with special polymers to give it greater staying power than conventional greases.  It has a blue colored smooth tacky appearance which readily identifies it from normal automotive grease products. This combination also makes it very resistant to water and gives it that special adherence to metallic surfaces.

Typical Properties

Appearance 						Smooth - Tacky

Thickener 						Lithium Complex

NLGI Grade 				      		1

Worked Penetration

@ 77 F ,    0.1mm			           325

Flash Point,  F					>500

Drop Point,  F					>500

Timken OK Load,  #					60

Special Additives					Polymers

Copper Corrosion,					1b