## SOLUTIONS PLUS CHEMICAL DATA

CLG-2

MULTI-PURPOSE GREASE

DESCRIPTION

CLG-2 is a lithium complex thickened grease fortified with a synthetic polymer that provides superior film strength and hence increased lubrication and protection to industrial equipment.  CLG-2 is a multi-purpose grease designed to be used in many different areas under many different conditions such as those found in Transportation, Automotive, Farming, Construction, Mining, Industrial, Food Processing, Packaging and Marine applications.

CLG-2 is an NLGI 1-1/2 grade grease which provides for better pumpability in remote grease applications.  The polymers incorporated into this high performance grease, increase the adhesiveness, shock load carrying ability and also its high load carrying ability adding to its outstanding performance.  The unique combination of polymers, extreme pressure and anti-wear additives make this a truly high performance lubricant.

ADVANTAGES

-Very adhesive (Tenacious)

-Polymers cushion shock loads

-Superior extreme pressure and anti-wear performance

-Excellent rust and oxidation resistance

SPECIFICATIONS

Color	:							Blue

Worked Penetration @ 77 Deg. F			300

Dropping Point, Deg. F					345

### Timken OK Load						60 lbs.

______________________________________________________________________________________

Solutions Plus Inc., 3907 Bach Buxton Road, Amelia, OH 45102

513-943-9600   Fax  513-943-9609