CHEMICAL DATA

# Multi Purpose Grease – 2G

Typical Properties

Color 						Green

Appearance 					Smooth - Tacky

Thickener 					Calcium Sulfonate Complex

NLGI Grade 				      		2

Worked Penetration

@ 77 F ,    0.1mm			           270

Worked 100,000 strokes,

Change in penetration,   0.1mm		2

Drop Point,  F					>550

Timken OK Load,  #					65

Special Additives					Polymers

4 Ball Wear Test,

Scar Diameter,  mm				0.39

4 Ball EP Test,

Weld Point , Kg					500

Rust Test						Pass

Oxidation Stability,  psi drop / 100 		0

Water Washout Test, ( 175º F )

% loss						2.75