# MT Gear Lube 6800

# Data Sheet

MT Gear Lube 6800 is a high performance, synthetic, heavy duty gear oil, designed for use in all types of enclosed gear boxes, open gears and plain and roller bearings calling for a very high viscosity lubricant.  The synthetic base stock of MT Gear Lube 6800 provides all of the advantages of a synthetic fluid: high viscosity index, low pour point, high flash point, outstanding oxidation stability, and superior performance at high and low temperatures.  The high performance additives in MT Gear Lube 6800 provide excellent rust and oxidation inhibition, gear scuffing protection and anti-wear performance. Its high viscosity makes MT Gear Lube 6800 an ideal candidate for slow speed, high load and high temperature applications.  It is an excellent lubricant for railroad traction motor drives.

Typical Properties

Viscosity, SUS @ 100°F			41,000

Viscosity, SUS @ 210°F			1825

Viscosity Index				180

Viscosity, cSt @ 40°C			8200

Pour Point, °F				+21

Flash Point, °F				446

Four Ball EP Test

Weld Load, Kg			250

Load Wear Index, Kgf		48

FZG test, Failure Stage			13+

MT Gear Lube 6800 is supplied in a 1.75# squeeze pouch for ease of application.