SOLUTIONS PLUS CHEMICAL DATA

METAL GARD 100 PLUS

General Description:

Metal Gard 100 Plus is a water emulsion type rust preventative. After application, the water evaporates and leaves behind a thin rust preventative film on the part. The Metal Gard 100 Plus can be applied directly to a steel or cast iron surfaces or used over zinc phosphate coatings for enhanced corrosion protection or as a break in lubricant. The Metal Gard 100 Plus can be diluted with water from 2% to 20% depending on the application to form a very stable emulsion. The Metal Gard 100 Plus is low foaming at all dilution rates and all temperatures. The product is formulated to control rancid odors and fungal growth in the diluted emulsion.

Indoor rust protection (1-2 years), good for high humidity environments- 500 + hours in humidity cabinet

Properties:

Color (Concentrate):				Clear Amber

Color (Emulsion):				Milky White

Specific Gravity:				0.928

Emulsion pH:					8.0 to 9.0

Using Procedures:

For indoor rust protection on steel and cast iron parts use the Metal Gard 100 Plus between 2% and 20%. The stronger the concentration, the better the rust protection. For use over zinc phosphate coatings use the Metal Gard 100 Plus between 5% and 12%. Heating the emulsion increases the drying time.

Concentration Control:

Use a Refractometer to control the concentration. The reading on the Refractometer indicates the concentration of the emulsion. For example; a 2 reading indicates a 2% concentration, a 10 reading indicates a 10% concentration and so on.

Solutions Plus, Inc. 3907 Bach Buxton Road, Amelia, OH 45102

513-943-9600  Fax-513-943-9600