Solutions Plus

Data Sheet

Prima Plus (For The Steel Industry)

Synthetic Gear Oil

Description

Prima Plus, gear oil is our highest quality synthetic polyglycol-based fluids. Prima Plus contains premium additives to withstand wear, oxidation, corrosion, extreme pressure and foam. Prima Plus lubricates where petroleum oil fails. Prima Plus solves gearbox problems. Prima Plus eliminates carbon residue, varnish and sludge caused by petroleum oxidation. Petroleum carbonizes at 200°F to 250°F. Prima Plus runs clean at hot spots of 350°F to 400°F +. PRIMA PLUS evaporates clean even when burned. Prima Plus has a long product life.

Prima Plus works extremely well in Mud Guns in the Steel Industry.  Prima Plus will cut, down/time, labor, replacement parts and costly repairs.

One major steel mill in USA have had huge success in eliminating wear and rebuilds on Mud Gun screw and plunger drives and tilt drives. Thousands of dollars have been saved.

Mud Gun

Key Properties

- reduces amperage: saves energy

- extends oil life: lowers disposal cost

- reduces wear: extends equipment life

- reduces temperature: extends oil life

- equipment stays cleaner: reduction of carbon and varnish deposits

- complete additive package

Prima Plus

Technical Data

Characteristics	ASTM    Prima Plus

| ISO Grade | D-2422 | 220 |  |
| --- | --- | --- | --- |
| AGMA* Grade |  | 5 |  |
| SAE Grade |  | 140 |  |
| Viscosity | D-445 |  |  |
| 40°C cSt |  | 232 |  |
| SUS |  | 1075 |  |
| 100°C cSt |  | 34.6 |  |
| SUS |  | 163 |  |
| 100°F SUS |  | 1183 |  |
| 210°F SUS |  | 167 |  |
| Viscosity Index | D-2270 | 197 |  |
| Flash Point, °F | D-92 | 475°F + |  |
| Pour Point, °F | D-97 | -28°F |  |
| Pounds/Gallon | D-287 | 8.37 |  |
| (FZG Wear Test,* |  |  |  |
| Stages Passed) |  | 12 |  |
| Rust Protection, A&B | D-665 | Pass |  |
| (Foam Suppression, |  |  |  |
| Seq. I, II, III) | D-892 | 0/0/0 |  |
| Copper Corrosion | D-130 | 1A |  |

Use Instructions

Check equipment manufacturers (OEM) viscosity requirements. For high temperature use, the best viscosity selection is SAE grade since SAE is based on the viscosity at 210°F.

*Prima Plus is an excellent extreme pressure (E.P.) lubricant. It passes the maximum 12 stages for an FZG wear test. AGMA requires only 11 stages for an E.P. oil. Prima can be used for all industrial gears, including worm gears.

Applications

Enclosed Gearboxes, Gear Reducers, Oil Lubricated Bearings, Chains, Transfer Cases and Mudd Guns.

Dispensing

Prima Plus is a liquid. Therefore, it can be withdrawn directly the shipping container by gravity or with conventional hand air-operated pumps.

Product Compatibility

Safe for use on ferrous and non-ferrous metals used in industrial equipment.

Test Method

Prima oils are not normally titrated.

Safe Handling and Storage Instructions
Keep container closed when not in use.  Store container side to prevent contamination. Inside storage is preferred.

Precautions

KEEP OUT OF THE REACH OF CHILDREN.

Please refer to the label and Material Safety Data information for all warnings, recommendations for safety equipment, other regulatory information. Copies of the Material Safety Data information can be ordered by calling 888-943-1100.

Disposal

Please refer to the Material Safety Data Sheet (MSDS) for instructions regarding proper disposal of this product.